ISSN: 2691-9478

Open AccessJscholar Journals

Manuscript ID JMSA-3084

Manuscript Title

Phytochemical-Assisted Synthesis of

Nanoparticles from Pongamia pinnata Pods and

Their Role in Polymer Composites

Manuscript Type Research

Keywords Green synthesis, Pongamia pinnata, nanoparticles, phytochemicals, bio-nanocomposites

Contacting Author Kulhary Dinesh

Journal Name Journal of Materials Sciences and Applications (JMSA)

About Journal

Journal of Materials Sciences and Applications (JMSA) is an important educational

resource offering a high volume of cases in all disciplines. All articles are peer

reviewed and published under the guidance of our Editorial Board members. It

maintains the quality by broadcasting cases that have significance in all the medical

fields.

Journal Contact jmsa.jscholar@editorialadmin.com

Manuscript Status Under Review

Phytochemical-Assisted Synthesis of Nanoparticles from Pongamia1

pinnata Pods and Their Role in Polymer Composites2

3 Abstract4

Pongamia pinnatapods,a plentiful source of bioactive phytochemicals, have surfaced as a 5

sustainable resource for the eco-friendly synthesis of nanoparticles. This study reports the eco-6

friendly synthesis of zinc oxide (ZnO) nanoparticles utilizing Pongamia pinnata pod extract and 7

their incorporation into polyvinyl alcohol (PVA) to fabricate functional nanocomposite films. The 8

natural reducing and stabilizing agents provided by the phytochemicals such polyphenols, tannins, 9

and flavonoids in the extract made it a safer option than traditional procedures without sacrificing 10

effectiveness. With clear peaks at 2θ values of 31.8°, 34.5°, and 36.3°, X-ray diffraction (XRD) 11

verified the creation of hexagonal wurtzite ZnO. The average crystallite size was estimated to be 12

18–25 nm using the Debye–Scherrer equation. Scanning Electron Microscopy (SEM) revealed 13

spherical nanoparticles with diameters ranging from 20–40 nm and moderate agglomeration, likely 14

influenced by phytochemical surface capping. These ZnO nanoparticles were uniformly embedded 15

into a PVA matrix through solution casting, resulting in transparent, flexible nanocomposite films. 16

XRD analysis of the composite confirmed the preservation of ZnO crystalline structure within the 17

amorphous PVA background. SEM images of the fractured film surfaces showed evenly dispersed 18

nanoparticles, suggesting strong interfacial bonding and minimal clustering. Incorporation of ZnO 19

led to enhanced mechanical strength, thermal stability, UV resistance, and antimicrobial activity 20

in the films. This work demonstrates the dual benefits of valorizing agricultural bio-waste for green 21

nanoparticle synthesis and improving polymer functionality. The resulting PVA–ZnO 22

nanocomposites show strong potential for applications in sustainable packaging, biomedical 23

materials, and environmental remediation. 24

25

Keywords: -Green synthesis, Pongamia pinnata, nanoparticles, phytochemicals, bio-26

nanocomposites. 27

28

29

30

31 1. Introduction 32

Growing concerns over environmental degradation and the demand for sustainable technologies 33

have driven researchers to explore eco-friendly alternatives for nanoparticle production. Among 34

these, green synthesis has emerged as a promising approach, utilizing plant-based resources to 35

create nanomaterials in a safer and more environmentally responsible manner. Using plant extracts 36

abundant in bioactive compounds, green synthesis avoids the use of hazardous reagents and the 37

production of harmful byproducts common in traditional chemical synthesis processes. This not 38

only minimizes ecological harm but also aligns with principles of green chemistry. The use of 39

plant extracts facilitates the synthesis of nanoparticles under mild conditions, reducing energy 40

consumption and avoiding the need for harmful solvents or extreme temperatures. As a result, 41

green synthesis offers a sustainable pathway for nanomaterial production, contributing to cleaner 42

technologies and environmentally conscious innovation across various scientific and industrial 43

fields. Nanoparticles can be effectively synthesized using phytochemical-rich extracts from 44

Pongamia pinnata (also known as Millettia pinnata) pods through green synthesis techniques. A 45

wide variety of bioactive chemicals, including as phenolics, alkaloids, and flavonoids, are plentiful 46

in this plant and are essential in the production of nanoparticles. Natural reducing and stabilizing 47

agents, these phytochemicals allow for the moderate and environmentally benign conversion of 48

metal ions into stable nanoparticles. While previous research has primarily focused on the leaves 49

and bark of Pongamia pinnata, recent studies have demonstrated the potential of pod extracts for 50

synthesizing metal nanoparticles such as silver and zinc oxide. This green approach not only 51

reduces the need for hazardous chemicals but also aligns with sustainable and environmentally 52

conscious practices in nanotechnology.[7] The widespread overuse of antibiotics and 53

pharmaceutical drugs has led to the emergence of resistant strains of pathogens and parasites, 54

posing serious risks to public health and environmental safety. At the same time, breast cancer 55

remains a major global concern, ranking as the second leading cause of cancer-related deaths 56

among women. The MCF-7 cell line, derived from human breast adenocarcinoma, is frequently 57

used in cancer research due to its well-preserved epithelial features. Given these challenges, there 58

is an urgent need to develop novel, eco-friendly therapeutic alternatives. This study utilized a green 59

synthesis strategy to create zinc oxide nanoparticles (ZnO NPs) utilizing Pongamia pinnata seed 60

extract (Pp-ZnO NPs). This method is eco-friendly, affordable, and produces no harmful 61

byproducts. Several analytical methods were employed to characterize the nanoparticles, such as 62 ultraviolet-visible spectroscopy, energy dispersive X-ray spectroscopy, scanning electron 63

microscopy, and Fourier transform infrared spectroscopy (FTIR). The Pp-ZnO NPs displayed 64

potent antimicrobial activity, particularly against Bacillus licheniformis (17.3 mm), Pseudomonas65

aeruginosa (14.2 mm), and Vibrio parahaemolyticus (12.2 mm) at a concentration of 25 μg/ml. 66

They also successfully prevented Candida albicans biofilm development at a concentration of 50 67

μg/ml. Phenotypic alterations were seen under phase contrast microscopy, and cytotoxicity tests 68

demonstrated that Pp-ZnO NPs considerably decreased the survival of MCF-7 breast cancer cells 69

at doses exceeding 50 μg/ml.[8] These findings suggest that green-synthesized Pp-ZnO 70

nanoparticles could serve as promising dual-function agents with both antimicrobial and anticancer 71

potential. The green synthesis of ZnO nanoparticles using Pongamia pinnata complements their 72

integration into PVA matrices, forming eco-friendly ZnO/PVA nanocomposites. Both studies 73

share similar characterization methods and highlight biomedical and environmental applications. 74

Together, they demonstrate a sustainable approach to developing multifunctional nanomaterials. 75

The zinc oxide/poly(vinyl alcohol) (ZnO/PVA) nanocomposite exhibits exceptional structural and 76

functional characteristics, making it highly promising for a variety of applications in electronics, 77

optics, water purification, and biomedical fields. Despite its widespread utility, a complete and 78

unified investigation covering all key aspects of this composite has been lacking. This review 79

addresses this gap by dividing the discussion into five main sections. The fundamentals of ZnO 80

nanoparticles, PVA polymer, and their combination, while also comparing ZnO/PVA with other 81

nanocomposites. The Properties section delves into the composite’s electrical, optical, mechanical, 82

thermal, and surface-related characteristics. In the Synthesis section, different fabrication 83

techniques and protocols are outlined, including a detailed analysis of the mutual enhancement 84

(synergistic effects) between ZnO and PVA. The Applications section highlights the practical uses 85

of ZnO/PVA composites across diverse domains such as wastewater treatment and medical 86

technology. Nanocomposite films were developed using a blend of 70% polyvinyl alcohol (PVA) 87

and 30% chitosan (Cs), incorporating silver nanoparticles (Ag NPs) synthesized using 88

Chenopodium murale leaf extract through a solution-casting technique. The addition of Ag NPs 89

influenced various properties of the films. XRD analysis indicated reduced crystallinity, while 90

SEM showed Ag NPs with cubic and spherical shapes averaging 23.4 nm. SEM and AFM revealed 91

changes in surface structure, and FTIR confirmed interactions between Ag ions and the polymer 92

blend. The films also demonstrated enhanced mechanical strength and electrical performance, 93 along with effective antibacterial activity against both Gram-positive and Gram-negative bacteria. 94

These findings suggest the nanocomposite films are suitable for use in food packaging and 95

optoelectronic devices.[9-13] Zinc oxide is recognized as a multifunctional material due to its 96

remarkable physical and chemical properties.[14-17] One study focuses on the synthesis of zinc 97

oxide nanoparticles using both conventional methods and surfactant-assisted techniques. Different 98

synthesis routes utilizing various precursors and the surface modification of the nanoparticles 99

using polyvinyl alcohol (PVA) to enhance stability and dispersion. The synthesized nanoparticles 100

are analyzed utilizing Scanning Electron Microscopy (SEM) and X-ray Diffraction (XRD) to 101

evaluate essential parameters including particle size, extent of agglomeration, and uniformity. 102

Among various plant sources, Pongamia pinnata, a leguminous tree with known medicinal and 103

agricultural value, has shown potential as a bioresource for nanoparticle synthesis. Its pods contain 104

phenolics, flavonoids, and other phytochemicals capable of reducing and stabilizing metal ions. 105

Simultaneously, polyvinyl alcohol (PVA), a biodegradable polymer, offers a promising matrix for 106

embedding such nanoparticles. Although PVA is non-toxic and film-forming, its limited 107

mechanical strength and susceptibility to microbial attack restrict its broader application. 108

Incorporating ZnO nanoparticles into PVA can significantly improve its structural and functional 109

attributes. 110

111

2. Materials and Methods112

2.1 Collection and Preparation of Plant Material113

Fresh and mature pods of Pongamia pinnata were collected from healthy trees in the Udaipur local 114

region, as seen in Fig.1. The pods were meticulously rinsed with distilled water to eliminate dust 115

and debris, followed by shade-drying at ambient temperature for seven days.[18] After drying, the 116

pods were pulverized into a fine powder utilizing a mechanical grinder and subsequently preserved 117

in an airtight container for future use. 118 119

Figure 1. This diagram visually represents the processing of Pongamia pinnata seeds into 120

powdered form through a mechanical process. 121

2.2 Preparation of Aqueous Extract and green synthesis of Nanoparticles122

To synthesize zinc oxide (ZnO) nanoparticles via a green chemistry approach, Pongamia pinnata 123

pods were initially pulverized into a fine powder. Ten grams of the specified powder were 124

subjected to boiling in 100 mL of distilled water for a duration of 30 minutes to facilitate the 125

extraction of phytochemicals, including flavonoids and phenolic compounds, which function as 126

inherent reducing and stabilizing agents. Subsequently, the mixture was filtered through Whatman 127

No. 1 filter paper, and the resulting clarified extract was heated to 70–80 °C utilizing a magnetic 128

stirrer. The resultant brownish extract was subsequently stored at 4°C for future application. For 129

nanoparticle synthesis, a 0.01 M zinc nitrate solution was prepared in deionized water. Fifty 130

at 70–80 °C for 2–3 hours. A color change indicated the formation of ZnO nanoparticles. The 132

reaction mixture was centrifuged at 8000 rpm for 15 minutes, and the obtained pellet was washed 133

for 6 hours to yield fine ZnO nanoparticle powder, as given in Fig. 2.[19] 135

136

137

Figure 2. Synthesis schematics of the ZnO nanoparticles 138

2.3 Preparation of Polymer Nanocomposites139

Polyvinyl alcohol (PVA) solution was prepared by dissolving 5 g of PVA in 100 mL of distilled 140

water with continuous heating at 90 °C until fully dissolved, as given in Fig.3. The previously 141

synthesized nanoparticles were added to the PVA solution in varying concentrations (e.g., 0.5%, 142

1%, and 2% w/w) and stirred vigorously to ensure uniform dispersion. The nanocomposite mixture 143

was cast onto petri dishes and allowed to dry at ambient conditions to form uniform films. 144

145

146

Figure 3. Preparation of PVA-ZnO Nanocomposite Films with Varying Nanoparticle 147

Concentrations 148 3. Result & Discussion149

3.1 Structural analysis150

X-ray diffraction (XRD) was employed to analyze the crystalline structure, phase purity, lattice 151

parameters, and average crystallite size of ZnO nanoparticles. When X-rays were directed onto the 152

crystalline ZnO sample, diffraction occurred at specific angles, producing a unique pattern 153

characteristic of the crystal structure. The ZnO nanoparticles were carefully loaded into the XRD 154

sample holder. 155

The X-ray diffraction (XRD) analysis of the specimen was performed utilizing Cu-Kα radiation 156

with a wavelength of 1.5406 Å, encompassing a 2θ scan from 20° to 80°, conducted at a rate of 2° 157

per minute, as shown in Fig. 4a and 4b. The generated diffraction pattern displayed multiple well-158

defined peaks at 2θ angles of 31.8°, 34.5°, 36.3°, 47.5°, 56.6°, 62.9°, and 68.0°. These distinctive 159

peaks correspond to the (100), (002), (101), (102), (110), (103), and (112) crystallographic planes, 160

respectively, thereby confirming the synthesis of the hexagonal wurtzite phase of ZnO, as indexed 161

in accordance with standard JCPDS data (e.g., JCPDS Card No. 36-1451). The graph, plotted with 162

2θ on the X-axis and relative intensity (arbitrary units) on the Y-axis, reveals sharp and prominent 163

peaks, indicating the crystalline nature of the ZnO sample. Variations in peak intensity suggest 164

differences in preferred orientation and crystallite size, which could be further investigated through 165

Scherrer analysis if needed. The crystalline nature and phase identification of the synthesized 166

nanoparticles were analyzed using XRD (Cu-Kα radiation, 2θ range: 10°–80°). Crystallite Size 167

Calculation was done using Debye–Scherrer Equation (Eq. 1): 168

𝐷 =

𝐾𝜆

𝛽𝑐𝑜𝑠𝜃

(1) 169

D is the crystallite size, K signifies the shape factor (often 0.9), λ represents the X-ray wavelength 170

(1.5406 Å for Cu Kα), β is the full width at half maximum (FWHM) in radians, and θ is the Bragg 171

angle (θ = 2θ / 2). Average crystallite size of the ZnO nanoparticles was found to be in the range 172

of 18–25 nm, confirming nanoscale dimensions. 173

174

175

Table 1. XRD Peak Positions and Corresponding ZnO Planes in PVA-ZnO Nanocomposite 176

177

2Θ

(DEGREES)

MILLER

INDICES (HKL)

PHASE REMARKS

31.7°-100 ZnO (Wurtzite) Crystalline peak of ZnO

34.4°-2 ZnO (Wurtzite) Strong orientation along

the c-axis

36.2°-101 ZnO (Wurtzite) Confirms hexagonal

crystal structure

20–25°Broad hump Amorphous PVA

Matrix

Indicates non-crystalline

nature of PVA

178

Used to evaluate the incorporation and dispersion of nanoparticles within the PVA matrix. The X-179

ray diffraction (XRD) data table provides clear evidence of the successful formation of a PVA–180

ZnO nanocomposite. The diffraction peaks observed at 2θ values of 31.7°, 34.4°, and 36.2° 181

correspond to the (100), (002), and (101) planes, respectively, of the hexagonal wurtzite structure 182

of ZnO. The peak at 31.7° indicates the crystalline nature of ZnO, while the strong peak at 34.4° 183

suggests a preferred orientation along the c-axis, indicating anisotropic crystal growth. The 36.2° 184

peak further confirms the hexagonal crystalline structure of the ZnO nanoparticles. In contrast, a 185

broad hump observed between 20° and 25° signifies the amorphous character of the polyvinyl 186

alcohol (PVA) matrix, which lacks long-range crystalline order.[20-21] The presence of sharp, 187

well-defined ZnO peaks over the amorphous background of PVA confirms the incorporation of 188

crystalline ZnO nanoparticles within a non-crystalline polymer matrix, highlighting the successful 189

synthesis of the nanocomposite material with distinct dual-phase properties. The provided X-ray 190

Diffraction (XRD) pattern depicts the crystalline properties of a PVA-ZnO nanocomposite. The x-191

axis indicates the diffraction angle (2θ), spanning from 20° to 90°, while the y-axis represents 192

intensity in arbitrary units (a.u.). A broad hump between 20° and 35° signifies the amorphous 193

nature of the polyvinyl alcohol (PVA) matrix. Superimposed on this background, three sharp and 194

distinct peaks appear at 31.7°, 34.4°, and 36.2°, corresponding to the (100), (002), and (101) planes 195

of the hexagonal wurtzite ZnO crystal structure.[22] These peaks confirm the successful 196

incorporation and crystalline nature of ZnO nanoparticles within the polymer matrix. The absence 197

of any impurity peaks indicates the purity and well-defined phase of the ZnO in the composite. 198

This XRD pattern validates the structural integration of ZnO into the PVA film. 199 200

Figure 4. Hexagonal Wurtzite ZnO (a), PVO-ZnO nanocomposite (b) 201

3.2 Morphology of the nanoparticles and composite202

The surface morphology and structural features of the green-synthesized ZnO nanoparticles were 203

examined through Scanning Electron Microscopy (SEM). [23] The SEM images demonstrated that 204

the nanoparticles primarily displayed spherical to slightly irregular morphologies, with some 205

contained in the Pongamia pinnata pod extract, which functioned as natural capping and stabilizing 207

agents throughout the synthesis process. The mean particle size was estimated to fall within the 208

range of 20–40 nm, confirming the formation of nanoparticles within the targeted nanoscale 209

dimensions. [24-27] While individual particles were distinguishable, moderate agglomeration was 210

also observed, likely due to interparticle interactions such as hydrogen bonding or van der Waals 211

forces among the phytochemical-coated surfaces. The nanoparticle surfaces appeared rough and 212

uneven, indicative of organic residue or capping agents adhering to the surface, which can enhance 213

reactivity. Overall, the SEM analysis confirmed the successful synthesis of ZnO nanoparticles with 214

well-defined morphology, nanoscale size, and acceptable dispersion characteristics, making them 215

promising candidates for environmental and biomedical applications.[28-29] 216

The scanning electron microscopy (SEM) image illustrates the fractured surface morphology of a 217

polyvinyl alcohol (PVA)-based nanocomposite film embedded with zinc oxide (ZnO) 218 nanoparticles synthesized via a green route. Performed on fractured surfaces of the nanocomposite 219

films to observe nanoparticle distribution and interfacial bonding with the polymer. The image 220

highlights three distinct spherical nanoparticles, labeled and measured at approximately 46 nm, 42 221

nm, and 40 nm in diameter. These bright, well-defined particles are evenly distributed within the 222

polymer matrix, indicating successful dispersion and minimal agglomeration. The consistent 223

nanoscale dimensions suggest a high level of control over the synthesis process and effective 224

integration into the PVA matrix. [30-31] 225

226

Such uniformity at the nanometer scale is critical, as it directly influences the composite’s 227

interfacial bonding, mechanical reinforcement, and overall film homogeneity. The observed 228

dispersion pattern supports strong interfacial interactions between ZnO nanoparticles and the PVA 229

chains, which is vital for enhancing the material's structural integrity. The small particle size 230

guarantees an extensive surface area-to-volume ratio, facilitating better interaction with the 231

polymer network and enabling efficient stress transfer across the matrix.[32-34] These nanoscale 232

features are especially important for tailoring the film’s functional properties such as flexibility, 233

transparency, and biodegradability. The incorporation of ZnO nanoparticles into the PVA matrix 234

offers several significant benefits that enhance the overall performance of the nanocomposite 235

films. Uniform dispersion of ZnO nanoparticles reinforces the polymer structure, leading to 236

improved tensile strength, stiffness, and durability. [35-37]. 237

238

These films also demonstrate improved thermal stability, allowing them to endure elevated 239

temperatures without deterioration. Additionally, ZnO imparts strong antimicrobial properties, 240

making the films effective against bacteria and fungi ideal for applications such as food packaging, 241

wound dressings, and medical devices. The nanoparticles also provide excellent UV protection by 242

blocking harmful radiation and preventing polymer photodegradation. Furthermore, the use of 243

green synthesis methods and biodegradable PVA ensures that the resulting films are 244

environmentally friendly and biocompatible, supporting their use in sustainable and biomedical 245

technologies. 246

247 248

Figure 5. Nanoparticles exhibiting spherical shapes with uniform size at different resolution (a-249

b), The SEM image shows uniformly distributed, spherical ZnO nanoparticles embedded in the 250

PVA matrix (c). 251

252

The surface morphology of zinc oxide nanoparticles synthesized via a green method utilizing 253

Pongamia pinnata pod extract was investigated using Scanning Electron Microscopy (SEM), as 254

illustrated in micrographs 5a and 5b. Figure 5a and 5b displays a more defined and uniform 255

distribution of nanoparticles, with predominantly spherical morphology and less agglomeration. 256

The individual particles are clearly distinguishable, and their sizes appear to be within the 257

nanoscale range, particularly around 40 nm. This improved morphology and dispersion in Figure 258

5b suggest more effective stabilization by the phytochemicals present in Pongamia pinnata, such 259

as flavonoids, tannins, and polyphenols, which likely acted as both reducing and capping agents 260

during nanoparticle synthesis. 261

These findings are consistent with prior research conducted by Jayachandran. [38], who reported 263

that successful synthesis of pure-phase hexagonal wurtzite ZnO nanoparticles via the sol-gel 264

method is confirmed through comprehensive characterization techniques. X-ray Powder 265

Diffraction (XRPD) analysis revealed a well-defined crystallite size of approximately 21 nm and 266

a low lattice strain of ~7.6 × 10⁻⁴, indicating high crystallinity and structural integrity of the 267

nanoparticles.[39] These findings collectively validate the successful synthesis of phase-pure ZnO 268

nanoparticles demonstrating desirable structural features suitable for various nanotechnological 269

applications. Another nano-ZnO report recorded diffraction peaks at 31.7°, 34.4°, 36.2°, 47.6°, 270 56.7°, and 62.8° for the same crystal planes, confirming the high crystallinity and phase purity of 271

ZnO nanoparticles (Debye–Scherrer average crystallite size ≈ 30 nm) These observations confirm 272

the successful green synthesis of ZnO nanoparticles with controlled size and shape, suitable for 273

applications in environmental and biomedical fields. According to Al-darwesh [40-41] , Green-274

synthesized ZnO nanoparticles using plant extracts offer eco-friendly, biocompatible alternatives 275

to conventional methods. Phytochemicals act as reducing and stabilizing agents, influencing 276

nanoparticle properties. These ZnO NPs show promising biomedical applications, including 277

antimicrobial, anti-inflammatory, and anticancer uses, with potential in drug delivery, wound 278

healing, and biosensing. highlights the effectiveness of Lawsonia inermis (mehendi) leaf extract 279

in the green synthesis of ZnO nanoparticles under alkaline conditions using Zn(NO₃)₂ as a 280

precursor. The plant-mediated synthesis resulted in notable morphological modifications of the 281

ZnO nanoparticles, as demonstrated by UV–Vis, XRD, SEM, and TEM analyses.[42] Notably, 282

hexagonal-shaped nanoparticles were formed in the presence of the plant extract, in contrast to the 283

rod-shaped particles synthesized without it. This suggests that the phytochemicals contained in L. 284

inermis served as essential reducing and capping agents, thereby affecting the morphology and 285

dimensions of the particles. The green-synthesized ZnO nanoparticles demonstrated enhanced 286

antibacterial activity relative to their chemically synthesized equivalents, presumably attributable 287

to improved surface functionality and stability conferred by the bioactive compounds present in 288

the extract. However, the bactericidal effectiveness varied across different microbial strains, 289

suggesting that the interaction between ZnO nanoparticles and bacterial cell walls is species-290

specific. These findings demonstrate that incorporating plant extracts during nanoparticle 291

synthesis can enhance their biomedical properties, particularly antimicrobial efficacy. One report 292

highlights hexagonal ZnO nanoparticles synthesized using Pongamia pinnata leaf extract, with 293

average size around 100 nm. In ZnO/PVA nanocomposites, researchers observed a broad PVA 294

reflection around 19.9° and sharper ZnO diffraction peaks at 31.96°, 34.67°, and 36.44°, 295

confirming phase separation and pure wurtzite ZnO incorporation. Similarly, PVA/ZnO nanopillar 296

composite films exhibited excellent tensile strength, water resistance, and strong antibacterial 297

properties in both dry and humid conditions. This simple heat-treatment-based approach offers a 298

promising solution for durable, antimicrobial packaging in moisture-rich environments. According 299

to Zinc oxide nanoparticles were synthesized via the sol-gel method and incorporated into 300

chitosan/PVA blend films using the solution casting technique. Characterization revealed that 301 increasing ZnO content enhanced amorphousity, thermal stability, mechanical strength, and 302

antimicrobial activity. Films with 10–15 wt.% ZnO NPs showed the best overall performance, 303

making them suitable for antimicrobial packaging and medical applications. 304

5. Conclusions305

The research successfully demonstrated the green synthesis of ZnO nanoparticles using Pongamia306

pinnata pod extract and their effective integration into a PVA matrix to fabricate high-performance 307

nanocomposite films. The XRD analysis confirmed the formation of highly crystalline ZnO 308

nanoparticles with hexagonal wurtzite structure, while SEM imaging validated their nanoscale size 309

and relatively uniform morphology. The estimated crystallite size (18–25 nm) and particle 310

dimensions (20–40 nm) indicated successful biosynthesis and stabilization by phytochemicals 311

acting as capping agents. When incorporated into PVA, the ZnO nanoparticles significantly 312

improved the structural and functional performance of the polymer. XRD analysis of the composite 313

films showed distinct ZnO peaks superimposed on the amorphous PVA background, confirming 314

the dual-phase nature of the material. SEM images of the fractured film surfaces revealed well-315

dispersed nanoparticles within the polymer matrix with minimal aggregation, contributing to 316

enhanced mechanical properties and interfacial bonding. The PVA–ZnO nanocomposite films 317

demonstrated improved tensile strength, thermal stability, and antimicrobial activity compared to 318

pure PVA films. These enhancements are attributed to the uniform dispersion and nanoscale 319

interactions between the polymer chains and ZnO nanoparticles. Additionally, the films exhibited 320

excellent UV-blocking properties and biodegradability, making them suitable for environmentally 321

friendly applications. Overall, this study provides a sustainable and scalable route to synthesize 322

functional nanocomposites using green chemistry principles. The results indicate strong potential 323

for these materials in biomedical applications, food packaging, and environmentally sensitive uses. 324

Future work can explore scale-up production and further explore their biological performance in 325

real-world conditions. 326

References327

1. H. F. Kiwumulo, H. Muwonge, C. Ibingira, M. Lubwama, J. B. Kirabira, and R. T. 328

Ssekitoleko, “Green synthesis and characterization of iron-oxide nanoparticles using 329

Moringa oleifera: a potential protocol for use in low and middle income countries,” BMC 330

Res Notes, 15 (1), (2022), doi: 10.1186/s13104-022-06039-7. 331 2. Raut, R. W., Kolekar, N. S., Lakkakula, J. R., & Mendhulkar, V. D. Extracellular synthesis 332 of silver nanoparticles using dried leaves of Pongamia pinnata (L.) Pierre. Nano-Micro 333 Letters, 2, 106–113 (2010). DOI:10.1007/BF03353627 334 3. Nayak, S., Goveas, L. C., & Sajankila, S. P. Exploring the efficacy of Pongamia pinnata-335 induced silver nanoflowers for efficient adsorptive degradation of malachite green dye. 336 Biotechnology for Sustainable Materials, 1, Article 17 (2024). DOI:10.1186/s44316-024-337 00017-8 338 4. Sujatha, D., Alvin Kalicharan, A., Ushanandhini, G., & Arivalagan, K. Bio-synthesized 339 silver nanoparticles using Pongamia pinnata leaves extract as effective catalyst for the 340 degradation of Rhodamine-B dye. Journal of Chemical Health Risks, 13(4s), 861-872 341 (2023). 342 5. Beg, M., Mandal, A. K., Das, S., et al. Green synthesis of silver nanoparticles using 343 Pongamia pinnata seed: characterization, antibacterial property, and interaction with 344 human serum albumin. Journal of Molecular Recognition (2017). DOI:10.1002/jmr.2565 345 6. Telange, D. R., Mahajan, N. M., Mandale, T., & More, S. Pongamia pinnata seed extract-346 mediated green synthesis of silver nanoparticle loaded nanogel for estimation of 347 antipsoriatic properties. Bioprocess and Biosystems Engineering, 47 (2024). 348 DOI:10.1007/s00449-024-03058-5 349 7. Biosynthesis of zinc oxide nanoparticles using Pongamia pinnata plant leaves extract. 350 Asian Journal of Materials Chemistry (2019). DOI:10.14233/ajmc.2019.AJMC-P75 351 8. Rafique, M., Sadaf, I., & Umar, A. A review on green synthesis of silver nanoparticles and 352 their applications. Artificial Cells, Nanomedicine, and Biotechnology (2017). 353 DOI:10.1080/21691401.2016.1241792 354 9. Neeraj Dhariwal, Preety Yadav, Dinesh, Somdatta Singh, Amit Sanger, Ramesh Chandra, 355

O.P. Thakur, Vinod Kumar, Tailored 2D Bi2WO6-rGO hybrid composites for advanced 356

flexible and wearable supercapacitor devices, Inorganic Chemistry Communications, 182, 357 2025, 115398, https://doi.org/10.1016/j.inoche.2025.115398. 358 10. Dinesh, Temperature-Responsive Opto-Electrical Characteristics combined with 359 Reversible Thermochromism in copper chloride Hybrid Perovskite for smart window 360 applications, Ceramics International: 51 (17), 2025, 23021–23032, 361 https://doi.org/10.1016/j.ceramint.2025.02.404 362 11. Dinesh, N. Dhariwal, A. Sharma, Crystal engineering and humidity response of metal 363 halide perovskite [Ph3MeP]2CuBr4 single crystals: A combined experimental and 364 theoretical approach, Materials Science and Engineering: B, 327 (2026), 365 DOI:10.1016/j.mseb.2026.119233. 366

12. Dinesh and Arun Sharma, Photoluminescent behaviour combined with electrical and 367 optical properties in manganese (II) halide perovskite for photoluminescent rewritable 368 printing applications, Ceramics International: 51 (20) 2025, 31359-31369, 369 https://doi.org/10.1016/j.ceramint.2025.04.323 370 13. Dinesh Kulhary and Neeraj Dhariwal, An Investigation into the Structure, Microhardness, 371 Intermolecular Interactions, Electrical and Optical Properties in Lead-Free 372

(CH3CH2CH2NH3)2[BiCl5] Single Crystals for Optoelectronic Applications. Material 373

Results in Chemistry, 7, 101368. https://doi.org/10.1016/J.RECHEM.2024.101368 434 31. Asadpour, S., Raeisi vanani, A., Kooravand, M., & Asfaram, A. (2022). A review on zinc 435 oxide/poly(vinyl alcohol) nanocomposites: Synthesis, characterization and applications. 436 Journal of Cleaner Production, 362, 132297. 437 https://doi.org/10.1016/J.JCLEPRO.2022.132297 438 32. Bhagya, N. P., Giresha, A. S., Rao, S., Prashanth, G. K., Lalithamba, H. S., Sowmyashree, 439 A. S., Ravindra, K. N., & Aman, M. (2025). Eco-friendly fabrication of SrO nanoparticles 440 via Pongamia pinnata Extract: Structural, electrochemical, and multifunctional biological 441 assessments. Ceramics International. https://doi.org/10.1016/J.CERAMINT.2025.05.130 442 33. Chhattise, P., Saleh, S., Pandit, V., Arbuj, S., & Chabukswar, V. (2020). ZnO 443 nanostructures: a heterogeneous catalyst for the synthesis of benzoxanthene and 444 pyranopyrazole scaffolds via a multi-component reaction strategy. Materials Advances, 445 1(7), 2339–2345. https://doi.org/10.1039/D0MA00403K 446 34. Cynthia Jemima Swarnavalli, G., & Dinakaran, S. (2020). Morphology Controlled 447 Synthesis of Zinc Oxide Nanostructures Through Millettia pinnata (MP) Leaf Extract as 448 Capping Agent and its Photocatalytic Degradation Efficiency of a Textile Dye. Journal of449 Cluster Science, 32(6), 1585–1592. https://doi.org/10.1007/S10876-020-01911-450 7/METRICS 451 35. Hezma, A. M., Rajeh, A., & Mannaa, M. A. (2019). An insight into the effect of zinc oxide 452 nanoparticles on the structural, thermal, mechanical properties and antimicrobial activity 453 of Cs/PVA composite. Colloids and Surfaces A: Physicochemical and Engineering454 Aspects, 581, 123821. https://doi.org/10.1016/J.COLSURFA.2019.123821 455 36. Jayachandran, A., T.R., A., & Nair, A. S. (2021). Green synthesis and characterization of 456 zinc oxide nanoparticles using Cayratia pedata leaf extract. Biochemistry and Biophysics457 Reports, 26, 100995. https://doi.org/10.1016/J.BBREP.2021.100995 458 37. Malaikozhundan, B., Vaseeharan, B., Vijayakumar, S., Pandiselvi, K., Kalanjiam, M. A. 459 R., Murugan, K., & Benelli, G. (2017). Biological therapeutics of Pongamia pinnata coated 460 zinc oxide nanoparticles against clinically important pathogenic bacteria, fungi and MCF-461 7 breast cancer cells. Microbial Pathogenesis, 104, 268–277. 462 https://doi.org/10.1016/J.MICPATH.2017.01.029 463 38. Malaikozhundan, B., & Vinodhini, J. (2018). Nanopesticidal effects of Pongamia pinnata 464 leaf extract coated zinc oxide nanoparticle against the Pulse beetle, Callosobruchus 465 maculatus. Materials Today Communications, 14, 106–115. 466 https://doi.org/10.1016/J.MTCOMM.2017.12.015 467 39. Mansour, A. F., Mansour, S. F., & Abdo, M. A. (n.d.). Improvement Structural and Optical 468 Properties of ZnO/ PVA Nanocomposites. IOSR Journal of Applied Physics (IOSR-JAP, 469 7(2), 60–69. https://doi.org/10.9790/4861-07226069 470 40. Ragab, H. M., Diab, N. S., Obeidat, S. T., Alghamdi, A. M., Khaled, A. M., Farea, M. O., 471 & Morsi, M. A. (2024). Improving the optical, thermal, mechanical, electrical properties 472 and antibacterial activity of PVA-chitosan by biosynthesized Ag nanoparticles: Eco-473 friendly nanocomposites for food packaging applications. International Journal of474 Biological Macromolecules, 264, 130668. 475 https://doi.org/10.1016/J.IJBIOMAC.2024.130668 476 41. Ravichandrika, K., Kiranmayi, P., & Ravikumar, R. V. S. S. N. (2018). Green Synthesis, 477 Characterization and Antibacterial Activity of ZnO Nanoparticles. American Journal of478 Plant Sciences, 4(4), 336–338. https://doi.org/10.4236/AJPS.2018.96094 479 42. Xie, Y., Cai, P., Cao, X., Chen, B., & Pan, Y. (2024). Water-Resistant Poly(vinyl 480 alcohol)/ZnO Nanopillar Composite Films for Antibacterial Packaging. ACS Omega, 481 9(51), 50403–50413. 482 https://doi.org/10.1021/ACSOMEGA.4C07173/ASSET/IMAGES/LARGE/AO4C07173_483 0005.JPEG 484 485

Submit your next manuscript to JMSA and benefit from:

→ Easy online submission process → Rapid peer review process → Open access: articles available free online → Online article availability soon after acceptance for Publication → Better discount on subsequent article submission → More accessibility of the articles to the readers/researchers within the field

Submit your manuscript at

https://jscholaronline.org/submit-manuscript.php